CERTIFICATE OF ANALYSIS

SECTION 1. PRODUCT AND COMPANY IDENTIFICATION

Product name: Cosmetic Grade Iridescent Red Glitter

Product code: FCH088	Batch Number: 20200408-C01 Production date: Apr. 01, 2020~ Apr.19, 2020

Expiry date:Apr.19, 2023

Supplier: Zhongshan Zhongtai Pigment Co., Ltd.

SECTION 2. INFORMATION ON SPECIFICATION

| Product Code | Color | Thickness | Solvent- resistance | Heat Resistance | Light/UV Resistance | Shape | size | FD&C Colorant | D&C Colorant | Pigment | PH Value | Surface Degradability |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| FCH088 | Iridescent Red | 36μm |  | 120~150℃ | 3.5 | Hexagon | 0.08mm-3.0mm |  | - | - | 7.0-7.5 |  |

SECTION 3. INFORMATION ON INGREDIENTS

| Key Ingredient | CAS NO. | EC NO. | Target% |
| --- | --- | --- | --- |
| Polybutylene Terephthalate | 26062-94-2 | 607-857-5 | 98.01 |
| Acrylates copolymer | 25133-97-5 | 607-559-5 | 1.3 |
| FD&C Red 40 (CI.16035) | 25956-17-6 | 247-368-0 | 0.53 |
| FD&C Yellow 5（CI.19140） | 1934-21-0 | 217-699-5 | 0.16 |

SECTION 4. TEST REPORT ON HEAVY METALS