SPECIFICATION

Coloron Pigment

(Code:RH893）

| Assay | Spec. Values | Test Method |
| --- | --- | --- |
| Calcium Aluminum Borosilicate | 92.0-95.0% | CRTM-51 |
| Ag | 5.0-8.0% | CRTM-48 |
| Particle Size | 100-600 µm | CRTM-42 |
| PH Value | 4.0-11.0 | CRTM-45 |
| Density: | 2.8-3.4g/cm3 | CRTM-47 |
| Oil absorption | 50-80g/100g | CRTM-46 |

Zhongshan Zhongtai Pigment Co.,Ltd

Website: http://www.zsztyl.com	E-mail: zhongtaiyanliao@163.com